BANGLADESH  UNIVERSITY OF ENGG. & TECHNOLOGY

###### GEOTECHNICAL ENGG. LABORATORY

##### HYDROMETER ANALYSIS

##### (For ASTM 152H Hydrometer)

| Student no. 1104111-1104115 |  | Group no. 3 | Date of test : 7-3-2015 |
| --- | --- | --- | --- |
| Description of soil : Sandy soil |  |  |  |
| Hydrometer No. : 152H |  | Specific gravity, Gs : 2.62 | Wt. of soil, Ws : 50 gm |
| R1 = 40 | L1 = 3.5 cm | Meniscus correction, Cm : 0.5 | Zero correction, Cz : 5 |
| R2 = 10 | L2 = 7.3 cm | Length of bulb, Lb : 17 cm | Volume of bulb, Vb : 50 cm3 |
| L = 16.18 – 0.1267RL |  |  | Area of Jar, Aj : 28.27 cm2 |
| Dispersing Agent & quantity used : 100 ml of standard solution |  |  |  |

| Date | Clock Time | Elapsed time, min | Temp C | Observed Hydrometer reading Ra | Hyd. Corr. Only for meniscus RL | Effective depth L cm | Unit wt. of water yw gm/cm3 | Viscosity of water n poise | Grain diameter D mm | Temperature correction Ct | Corrected Hyd. Reading. Rc | % Finer (% of portion finer than #200 sieve only) N | % Finer (combined) Nc |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 |
| 7-3-2015 | 3:17 PM | .25 | 25 | 50 | 50.5 | 9.78 | .9971 | .00895 | .081 | +1.30 | 46.8 | 94.25 | .24 |
|  | 3:17 PM | .5 | 25 | 49 | 49.5 | 9.9 | .9971 | .00895 | .058 | +1.30 | 45.8 | 92.23 | .23 |
|  | 3:18 PM | 1 | 25 | 46 | 46.5 | 10.28 | .9971 | .00895 | .042 | +1.30 | 42.8 | 86.19 | .22 |
|  | 3:19 PM | 2 | 25 | 40 | 40.5 | 11.04 | .9971 | .00895 | .031 | +1.30 | 36.8 | 74.11 | .19 |
|  | 3:21 PM | 4 | 25 | 35 | 35.5 | 11.68 | .9971 | .00895 | .022 | +1.30 | 31.8 | 64.03 | .16 |
|  | 3:25 PM | 8 | 25 | 31 | 31.5 | 12.2 | .9971 | .00895 | .016 | +1.30 | 27.8 | 55.98 | .14 |
|  | 3:32 PM | 15 | 25 | 20 | 20.5 | 13.6 | .9971 | .00895 | .012 | +1.30 | 16.8 | 33.83 | .085 |
|  | 3:47 PM | 30 | 25 | 2 | 2.5 | 15.9 | .9971 | .00895 | .0095 | +1.30 | -1.2 | 2.41 | .006 |
|  | 4:17 PM | 60 | 25 | 0 | .5 | 16.13 | .9971 | .00895 | .0068 | +1.30 | -3.2 | 6.44 | .0161 |